|  |  | Woochang Chemical Co., LTD. |
| --- | --- | --- |
|  | Technical Bulletin |  |
| DLP (Dibasic Lead Phosphite) |

# 1. TYPE & COMPONENT

- Dibasic Lead Phosphite(2PbO.PbHPO3.1/2H2O)

# 2. TYPICAL PROPERTIES

| Appearance | : | White Powder |
| --- | --- | --- |
| Volatile Matter(105℃) | : | Max. 0.5 % |
| Lead Content(%) | : | 80.5 ~ 83.5 % |
| Mesh(325mesh) | : | Min. 99.0 % |
| Free Acid | : | Max. 0.50 mgKOH/g |

# 3. STANDARD PACKAGE

- 25Kg Paper Bag

- 500Kg Bulk Bag

# 4. FEATURE & USAGES

- Good static heat-stability for PVC

- Good initial color, heat-stability, superior insulation resistance.

# 5. SPECIFICATION

# - DLP is Dibasic Lead Phosphite. It’s a representative product for kind of lead

# stabilizer for PVC. It is widely used for both flexible and rigid products and mainly used for

# PVC compound due to its outstanding function as an insulator. Superior heat stability and

# UV stability.

# 6. HANDLING AND STORAGE

- DLP is Single PVC stabilizer and should be handled with normal precautions used in good

industrial practices. Store in cool, dry area. Indoor storage is recommendable.

# Text boxes

# WOOCHANG CHEMICAL CO., LTD.

223-34,  Whanseong-ri,  Jikok-myeon,  Seosan-si,  Chungcheongnam-do,  Rep of Korea

TEL : +82 41 664 6671  FAX : +82 41 669 6638